## Slide 1: MSE 3109: Kinetic Process in Engineering Materials
Instructor: Yuntian Zhu
Office: R7182, Ph: 3442-2457
y.zhu@cityu.edu.hk
Lecture 2: Diffusion II
Notes: Text book,
Office hour, by appointment

## Slide 2: Substitutional diffusion
Self Diffusion (substitutional):
Q is roughly proportional to Tm:
Q/Tm ~ constant for a fixed structure (Table 2.2,p83)
D
Interstitial diffusion
Dilute solution:
DA
Xv is the vacancy fraction
=
DGm = DHm -TDSm
DGv = DHv -TDSv
Q = DHm + DHv
Notes: The zXv = available positions for the atom to jump for substitutional diffusion
Quiz: Why Q/Tm ~ constant?
Why bcc metal has higher D0?

## Slide 3: Vacancy diffusion
Self Diffusion:
=
=
DA = DVXV
Same flux, different diffusion Coefficient
For self or substitutional diffusion
Diffusion of atoms is equivalent of diffusion of vacancy to the opposite direction (flux)
Diffusion coefficient of vacancy diffusion is much higher than that of atom diffusion
XV = 10-4 – 10-3 at Tm

## Slide 4: Diffusion in Substitutional Alloys
Darken’s equation
is roughly constant at Tm
bcc lattice has higher diffusion coefficient than fcc lattice
For dilute solution:
A and B form an alloy
Notes: Quiz: Why bcc lattice has higher diffusion coefficient? Density low
XA ->1, XB->0,

## Slide 5: Kirkendall Effect
A B
Cu-Zn Alloy
C0 =CA+ CB
JA = -(JB + JV),
JA
JB
JV
Notes: DA > DB, DZn > Dcu C = n/V, Fig. 2.15 on page 88
Quiz: Why an element with lower Tm has higher D?

## Slide 6: Factors affecting Diffusion direction
Strain field: Diffusion to GB and dislocations
  Implications:
Electric field
Notes: Quiz: Can the diffusion happen if there is no composition gradient?
Diffusion of the pure metal under bending stress?

## Slide 7: Diffusion along Grain Boundaries
Temperature effect on Diffusion mechanism
Transition T=0.75-0.8 Tm
Fig. 25
Qb ~ 0.5 Ql
d+d d
D=D0exp(-Q/RT)
logD=logD0-Q/RT
Notes: Qb ~ 0.5 Ql
At low T: GB diffusion dominates
At high T: Lattice diffusion dominates

## Slide 8: Diffusion along Dislocations
Notes: g = 10-10
May become significant at low T, Derivation similar to GB effect

## Slide 9: Diffusion in Multiphase Binary System
a
b
c
d
e
f
g
h
X (Zn)
a
b
c
d
e
f
g
h
Zn
A3
CuZn-Brass
B2
A1
Composition profile during diffusion
Notes: Draw the depth-composition profile
Why there is no two-phase zone along the depth (dG/dx = 0 at two phase equilibrium prevents diffusion, no driving force)
Use an eutectic system for demo

## Slide 10: Interface speed
Notes: Fig. 2.30

## Slide 11: Home Work
Reading assignment:
  Chapter 2.3-2.8 “Phase Transformations in Metals and Alloys”, David A. Porter et al.
HW: 2.9,